GUANZHOU KAIHENG K&S CO.,LTD.

Address:NO.148,Chang'an,Guangshan Road,Huangpu District,Guangzhou,China

TEL:+86-20-3207 9090              FAX:+86-20-3207 9103

E-mail:angel@gzkaiheng.com         URL:www.gzkaiheng.com

weChat / QQ:68118858              Skype:fengfengzhou

Mobile phone/whatsApp:+86-13416189912

KOSOO K-2(HF)

Halogen free, low smoking, flame-retardant polyolefin tubing

- Application

KOSOO K-2(HF) is halogen free, low smoking, flame-retardant irradiated crosslinking polyolefin heat-shrinkable tubing suitable for environmentally friendly application. It contains no added halogens, and exhibits excellent fire safety characteristics combined with low evolution of acid gases, while retaining good mechanical and fluid resistance properties.

- Features/Benefits

·Shrink ratio: 2:1.

·Flexible, flame-retardant.

·Low smoking, no added halogens.

·Low evolution of acid gases.

·Free of PCBs, PCPs, polybrominated biphenyls (PBBs), polybrominated biphenyl oxides and ethers (PBBOs, PBBEs and PBDEs) and toxic heavy metal compounds, which are classified as environmentally hazardous substances. Conform to European RoHS environmental directive.

- Operating Temperature Range

Operating temperature range: -55℃~125℃

Minimum shrink temperature: 70℃

Minimum full recovery temperature: 110℃

- Standards/Approvals

UL224 E214175 125℃ 600V VW-1

- Specification values

|  | Property | Requirement | Test method | Typical data |
| --- | --- | --- | --- | --- |
| Physical： | Concentricity | 70% min. | ASTM D 2671 | ≥70% |
|  | Tensile strength | 10.4MPa min. | ASTM D 638 | ≥12MPa |
|  | Elongation | 200% min. | ASTM D 638 | ≥300% |
|  | Heat shock | No cracking, dripping or flowing | ASTM D 2671 | Pass |
|  | Low temperature flexibility | No cracking | ASTM D 2671 | Pass |
|  | Aging 158℃,168hrs |  |  |  |
|  | Tensile strength after aging | 70% of original min. | ASTM D 638 | ≥80% |
|  | Elongation after aging | 100% min. | ASTM D 638 | ≥200% |
| Electrical： | Dielectric voltage withstand | 2500V, 60sec no breakdown | UL224 | Pass |
|  | Dielectric strength | 19.7KV/mm min. | ASTM D 2671 | 25KV/mm |
|  | Volume resistivity | 1014Ω·cm min. | ASTM D 876 | ≥1014Ω·cm |
| Chemical： | Corrosion | No corrosion | ASTM D 2671 | Pass |
|  | Flammability | VW-1 | UL224 | Pass |

- Product sizes

·Inch size                                                               mm/inch

| Size | Inside diameter | Wall thickness | Standard length (m/spool) |
| --- | --- | --- | --- |
|  | As supplied(min.) | After recovery(max.) | After recovery |  |
| 3/64 | 1.2（0.046） | 0.6（0.023） | 0.40±0.08（0.016±0.003） | 200 |
| 1/16 | 1.6（0.063） | 0.8（0.031） | 0.43±0.08（0.017±0.003） | 200 |
| 3/32 | 2.4（0.093） | 1.2（0.046） | 0.51±0.08（0.020±0.003） | 200 |
| 1/8 | 3.2（0.125） | 1.6（0.062） | 0.51±0.08（0.020±0.003） | 200 |
| 3/16 | 4.8（0.187） | 2.4（0.093） | 0.51±0.08（0.020±0.003） | 100 |
| 1/4 | 6.4（0.250） | 3.2（0.125） | 0.64±0.08（0.025±0.003） | 100 |
| 3/8 | 9.5（0.375） | 4.8（0.187） | 0.64±0.08（0.025±0.003） | 100 |
| 1/2 | 12.7（0.500） | 6.4（0.250） | 0.64±0.08（0.025±0.003） | 100 |
| 3/4 | 19.1（0.750） | 9.5（0.375） | 0.76±0.08（0.030±0.003） | 50 |
| 1 | 25.4（1.000） | 12.7（0.500） | 0.89±0.12（0.035±0.005） | 50 |
| 1 1/4 | 31.8（1.250） | 15.9（0.625） | 1.02±0.15（0.040±0.006） | 50 |
| 1 1/2 | 38.1（1.500） | 19.1（0.750） | 1.02±0.15（0.040±0.006） | 50 |
| 2 | 50.8（2.000） | 25.4（1.000） | 1.14±0.16（0.045±0.007） | 50 |

·Metric size

| Size(mm) | As supplied(mm) | After recovery (mm) | Standard length (m/spool) |
| --- | --- | --- | --- |
|  | Inside diameter | Wall thickness | Inside diameter（max.） | Wall thickness（min.） |  |
| Φ0.8 | 1.0±0.2 | 0.15±0.05 | 0.50 | 0.25 | 200 |
| Φ1.0 | 1.5±0.3 | 0.20±0.05 | 0.60 | 0.33 | 200 |
| Φ1.5 | 2.0±0.3 | 0.20±0.05 | 0.75 | 0.36 | 200 |
| Φ2.0 | 2.5±0.3 | 0.20±0.05 | 1.00 | 0.44 | 200 |
| Φ2.5 | 3.0±0.3 | 0.25±0.05 | 1.25 | 0.44 | 200 |
| Φ3.0 | 3.5±0.3 | 0.25±0.05 | 1.50 | 0.44 | 200 |
| Φ3.5 | 4.0±0.3 | 0.25±0.05 | 1.75 | 0.44 | 200 |
| Φ4.0 | 4.5±0.3 | 0.25±0.05 | 2.00 | 0.44 | 200 |
| Φ4.5 | 5.0±0.3 | 0.25±0.05 | 2.25 | 0.44 | 200 |
| Φ5.0 | 5.5±0.3 | 0.28±0.05 | 2.50 | 0.56 | 100 |
| Φ6.0 | 6.5±0.3 | 0.28±0.05 | 3.00 | 0.56 | 100 |
| Φ7.0 | 7.6±0.3 | 0.30±0.07 | 3.50 | 0.56 | 100 |
| Φ8.0 | 8.6±0.3 | 0.30±0.07 | 4.00 | 0.56 | 100 |
| Φ9.0 | 9.6±0.3 | 0.30±0.07 | 4.50 | 0.56 | 100 |
| Φ10.0 | 10.7±0.4 | 0.30±0.07 | 5.00 | 0.56 | 100 |
| Φ11.0 | 11.7±0.4 | 0.30±0.07 | 5.50 | 0.56 | 100 |
| Φ12.0 | 12.7±0.4 | 0.30±0.07 | 6.00 | 0.56 | 100 |
| Φ13.0 | 13.7±0.4 | 0.35±0.08 | 6.50 | 0.69 | 100 |
| Φ14.0 | 14.7±0.4 | 0.35±0.08 | 7.00 | 0.69 | 100 |
| Φ15.0 | 15.7±0.5 | 0.35±0.08 | 7.50 | 0.69 | 100 |
| Φ16.0 | 16.7±0.5 | 0.35±0.08 | 8.00 | 0.69 | 100 |
| Φ18.0 | 19.0±0.5 | 0.40±0.10 | 9.00 | 0.77 | 100 |
| Φ20.0 | 21.0±0.5 | 0.40±0.10 | 10.00 | 0.77 | 50 |
| Φ22.0 | 23.0±0.5 | 0.40±0.10 | 11.00 | 0.77 | 50 |
| Φ25.0 | 26.0±1.0 | 0.45±0.10 | 12.50 | 0.87 | 50 |
| Φ28.0 | 29.0±1.0 | 0.45±0.10 | 14.00 | 0.87 | 50 |
| Φ30.0 | 31.5±1.0 | 0.45±0.10 | 15.00 | 0.87 | 50 |
| Φ35.0 | 36.5±1.0 | 0.50±0.10 | 17.50 | 0.97 | 50 |
| Φ40.0 | 41.5±1.0 | 0.50±0.10 | 20.00 | 0.97 | 50 |
| Φ50.0 | 51.5±1.0 | 0.55±0.10 | 25.00 | 0.97 | 50 |
| Φ60.0 | 63.0±3.0 | 0.60±0.15 | 30.00 | 1.17 | 25 |
| Φ70.0 | 71.0±3.0 | 0.60±0.15 | 35.00 | 1.17 | 25 |
| Φ80.0 | 81.0±3.0 | 0.65±0.15 | 40.00 | 1.20 | 25 |
| Φ90.0 | 91.0±3.0 | 0.75±0.15 | 45.00 | 1.30 | 25 |
| Φ100 | 101.0±3.0 | 0.75±0.15 | 50.0 | 1.30 | 25 |
| Φ120 | 121.0±4.0 | 0.80±0.20 | 60.0 | 1.40 | 15 |
| Φ150 | 151.0±4.0 | 0.80±0.20 | 75.0 | 1.50 | 15 |
| Φ180 | 181.0±4.0 | 0.85±0.20 | 90.0 | 1.60 | 15 |

- Ordering Information

# Color                                             Standard packaging

Standard: Black (-BK), white (-WH)                    On spools. Cut pieces are available upon request.

Nonstandard: Available upon request.

# Nonstandard size                                   Ordering description

Special sizes are available upon request                  Specify product type, size (mm or inch) and color.