GUANZHOU KAIHENG K&S CO.,LTD.

Address:NO.148,Chang'an,Guangshan Road,Huangpu District,Guangzhou,China

TEL:+86-20-3207 9090              FAX:+86-20-3207 9103

E-mail:angel@gzkaiheng.com         URL:www.gzkaiheng.com

weChat / QQ:68118858              Skype:fengfengzhou

Mobile phone/whatsApp:+86-13416189912

KOSOO K-2

Environment friendly, flexible, flame-retardant polyolefin tubing

- Application

KOSOO K-2 is environment friendly, flexible, flame-retardant, irradiated crosslinking heat-shrinkable modified polyolefin tubing. Unlike other typical flame-retarant tubings, K-2 is free of PCBs, PCPs, polybrominated biphenyls (PBBs), polybrominated biphenyl oxides and ethers (PBBOs, PBBEs and PBDEs) and toxic heavy metal compounds, which are classified as environmentally hazardous substances. This high-reliability product is widely used for insulation or jacketing of wire harness, strain relief of wire terminations and connections, bundling of wire harness, protection of soldered points, insulation and capsule of electronic components, anti-corrosive protection, identification and color coding, etc.

- Features/Benefits

·Shrink ratio: 2:1.

·Very flexible, highly flame-retardant.

·Low shrink temperature.

·Good thermal stability.

·Excellent physical, chemical and electrical properties.

·Free of PCBs, PCPs, polybrominated biphenyls (PBBs), polybrominated biphenyl oxides and ethers (PBBOs, PBBEs and PBDEs) and toxic heavy metal compounds, which are classified as environmentally hazardous substances. Conform to European RoHS environmental directive.

·Wide range of sizes and colors.

- Operating Temperature Range

Operating temperature range: -55℃~135℃

Minimum shrink temperature: 70℃

Minimum full recovery temperature: 110℃

- Standards/Approvals

UL224 E214175 125℃ 600V VW-1

AMS-DTL-23053/5 class 1 and class 2

- Specification values

|  | Property | Requirement | Test method | Typical data |
| --- | --- | --- | --- | --- |
| Physical： | Concentricity | 70% min. | ASTM D 2671 | ≥70% |
|  | Tensile strength | 10.4MPa min. | ASTM D 638 | ≥14.0MPa |
|  | Elongation | 200% min. | ASTM D 638 | ≥400% |
|  | Heat shock | No cracking, dripping or flowing | ASTM D 2671 | Pass |
|  | Low temperature flexibility | No cracking | ASTM D 2671 | Pass |
|  | Aging 158℃, 168hrs |  |  |  |
|  | Tensile strength after aging | 70% of original min. | ASTM D 638 | ≥90% |
|  | Elongation after aging | 100% min. | ASTM D 638 | ≥300% |
| Electrical： | Dielectric voltage withstand | 2500V, 60sec no breakdown | UL224 | Pass |
|  | Dielectric strength | 19.7KV/mm min. | ASTM D 2671 | 25KV/mm |
|  | Volume resistivity | 1014Ω·cm min. | ASTM D 876 | ≥1014Ω·cm |
| Chemical： | Corrosion | No corrosion | ASTM D 2671 | Pass |
|  | Flammability | VW-1 | UL224 | Pass |

- Product sizes

·Inch size                                                          mm/inch

| Size | Inside diameter | Wall thickness | Standard length (m/spool) |
| --- | --- | --- | --- |
|  | As supplied (min.) | After recovery (max.) | After recovery |  |
| 3/64 | 1.2（0.046） | 0.6（0.023） | 0.40±0.08（0.016±0.003） | 200 |
| 1/16 | 1.6（0.063） | 0.8（0.031） | 0.43±0.08（0.017±0.003） | 200 |
| 3/32 | 2.4（0.093） | 1.2（0.046） | 0.51±0.08（0.020±0.003） | 200 |
| 1/8 | 3.2（0.125） | 1.6（0.062） | 0.51±0.08（0.020±0.003） | 200 |
| 3/16 | 4.8（0.187） | 2.4（0.093） | 0.51±0.08（0.020±0.003） | 100 |
| 1/4 | 6.4（0.250） | 3.2（0.125） | 0.64±0.08（0.025±0.003） | 100 |
| 3/8 | 9.5（0.375） | 4.8（0.187） | 0.64±0.08（0.025±0.003） | 100 |
| 1/2 | 12.7（0.500） | 6.4（0.250） | 0.64±0.08（0.025±0.003） | 100 |
| 3/4 | 19.1（0.750） | 9.5（0.375） | 0.76±0.08（0.030±0.003） | 50 |
| 1 | 25.4（1.000） | 12.7（0.500） | 0.89±0.12（0.035±0.005） | 50 |
| 1 1/4 | 31.8（1.250） | 15.9（0.625） | 1.02±0.15（0.040±0.006） | 50 |
| 1 1/2 | 38.1（1.500） | 19.1（0.750） | 1.02±0.15（0.040±0.006） | 50 |
| 2 | 50.8（2.000） | 25.4（1.000） | 1.14±0.16（0.045±0.007） | 50 |
| 5/2 | 63.5（2.500） | 31.8（1.250） | 1.27±0.20（0.050±0.008） | 25 |
| 3 | 76.0（3.000） | 38.1（1.500） | 1.27±0.20（0.050±0.008） | 25 |
| 4 | 101.6（4.000） | 50.8（2.000） | 1.40±0.23（0.055±0.009） | 25 |
| 5 | 127.0（5.000） | 63.5（2.500） | 1.52±0.23（0.060±0.009） | 15 |
| 6 | 147.0（5.787） | 75.0（2.953） | 1.70±0.25（0.067±0.010） | 15 |
| 8 | 200.0（7.874） | 100.0（3.937） | 1.90±0.28（0.075±0.011） | - |

·Metric size

| Size (mm) | As supplied (mm) | After recovery (mm) | Standard length (m/spool) |
| --- | --- | --- | --- |
|  | Inside diameter | Wall thickness | Inside diameter (max.) | Wall thickness (min.) |  |
| Φ0.8 | 1.0±0.2 | 0.15±0.05 | 0.50 | 0.25 | 200 |
| Φ1.0 | 1.5±0.3 | 0.20±0.05 | 0.60 | 0.33 | 200 |
| Φ1.5 | 2.0±0.3 | 0.20±0.05 | 0.75 | 0.36 | 200 |
| Φ2.0 | 2.5±0.3 | 0.20±0.05 | 1.00 | 0.44 | 200 |
| Φ2.5 | 3.0±0.3 | 0.25±0.05 | 1.25 | 0.44 | 200 |
| Φ3.0 | 3.5±0.3 | 0.25±0.05 | 1.50 | 0.44 | 200 |
| Φ3.5 | 4.0±0.3 | 0.25±0.05 | 1.75 | 0.44 | 200 |
| Φ4.0 | 4.5±0.3 | 0.25±0.05 | 2.00 | 0.44 | 200 |
| Φ4.5 | 5.0±0.3 | 0.25±0.05 | 2.25 | 0.44 | 200 |
| Φ5.0 | 5.5±0.3 | 0.28±0.05 | 2.50 | 0.56 | 100 |
| Φ6.0 | 6.5±0.3 | 0.28±0.05 | 3.00 | 0.56 | 100 |
| Φ7.0 | 7.6±0.3 | 0.30±0.07 | 3.50 | 0.56 | 100 |
| Φ8.0 | 8.6±0.3 | 0.30±0.07 | 4.00 | 0.56 | 100 |
| Φ9.0 | 9.6±0.3 | 0.30±0.07 | 4.50 | 0.56 | 100 |
| Φ10.0 | 10.7±0.4 | 0.30±0.07 | 5.00 | 0.56 | 100 |
| Φ11.0 | 11.7±0.4 | 0.30±0.07 | 5.50 | 0.56 | 100 |
| Φ12.0 | 12.7±0.4 | 0.30±0.07 | 6.00 | 0.56 | 100 |
| Φ13.0 | 13.7±0.4 | 0.35±0.08 | 6.50 | 0.69 | 100 |
| Φ14.0 | 14.7±0.4 | 0.35±0.08 | 7.00 | 0.69 | 100 |
| Φ15.0 | 15.7±0.5 | 0.35±0.08 | 7.50 | 0.69 | 100 |
| Φ16.0 | 16.7±0.5 | 0.35±0.08 | 8.00 | 0.69 | 100 |
| Φ18.0 | 19.0±0.5 | 0.40±0.10 | 9.00 | 0.77 | 100 |
| Φ20.0 | 21.0±0.5 | 0.40±0.10 | 10.00 | 0.77 | 50 |
| Φ22.0 | 23.0±0.5 | 0.40±0.10 | 11.00 | 0.77 | 50 |
| Φ25.0 | 26.0±1.0 | 0.45±0.10 | 12.50 | 0.87 | 50 |
| Φ28.0 | 29.0±1.0 | 0.45±0.10 | 14.00 | 0.87 | 50 |
| Φ30.0 | 31.5±1.0 | 0.45±0.10 | 15.00 | 0.87 | 50 |
| Φ35.0 | 36.5±1.0 | 0.50±0.10 | 17.50 | 0.97 | 50 |
| Φ40.0 | 41.5±1.0 | 0.50±0.10 | 20.00 | 0.97 | 50 |
| Φ50.0 | 51.5±1.0 | 0.55±0.10 | 25.00 | 0.97 | 50 |
| Φ60.0 | 63.0±3.0 | 0.60±0.15 | 30.00 | 1.17 | 25 |
| Φ70.0 | 71.0±3.0 | 0.60±0.15 | 35.00 | 1.17 | 25 |
| Φ80.0 | 81.0±3.0 | 0.65±0.15 | 40.00 | 1.20 | 25 |
| Φ90.0 | 91.0±3.0 | 0.75±0.15 | 45.00 | 1.30 | 25 |
| Φ100 | 101.0±3.0 | 0.75±0.15 | 50.0 | 1.30 | 25 |
| Φ120 | 121.0±4.0 | 0.80±0.20 | 60.0 | 1.40 | 15 |
| Φ150 | 151.0±4.0 | 0.80±0.20 | 75.0 | 1.50 | 15 |
| Φ180 | 181.0±4.0 | 0.85±0.20 | 90.0 | 1.60 | 15 |

- Ordering Information

# Color

Standard: Black (-BK), white (-WH), red (-RD), blue (-BL), yellow (-YL), green (-GR)

Nonstandard: Brown (- BR), orange (-OR), violet (-VT), gray (-GY), yellow & green stripe (-GYS)

# Nonstandard size

Special sizes are available upon request.

# Standard packaging

On spools. Cut pieces are available upon request.

# Ordering description

Specify product type, size (mm or inch) and color.