GUANZHOU KAIHENG K&S CO.,LTD.

Address:NO.148,Chang'an,Guangshan Road,Huangpu District,Guangzhou,China

TEL:+86-20-3207 9090              FAX:+86-20-3207 9103

E-mail:angel@gzkaiheng.com         URL:www.gzkaiheng.com

weChat / QQ:68118858              Skype:fengfengzhou

Mobile phone/whatsApp:+86-13416189912

KOSOO K-2(CB) THIN WALL

Environment friendly, ultra thin-wall, flexible, flame-retardant, polyolefin tubing

- Application

KOSOO K-2 (CB) is environment friendly, ultra thin-wall, flexible, flame-retardant, irradiated crosslinking heat-shrinkable modified polyolefin tubing. It is designed for applications that require an ultra thin wall for rapid shrinking and space saving. Low shrink temperature further reduces installation time and the risk of damage to temperature-sensitive components.

- Features/Benefits

·Shrink ratio: 2:1

·Low shrink temperature.

·Ultra thin-wall, rapid shrinking.

·Very flexible, flame-retardant.

·Free of PCBs, PCPs, polybrominated biphenyls (PBBs), polybrominated biphenyl oxides and ethers (PBBOs, PBBEs and PBDEs) and toxic heavy metal compounds, which are classified as environmentally hazardous substances. Conform to European RoHS environmental directive.

·Wide range of sizes and colors.

- Operating Temperature Range

Operating temperature range: -55℃~125℃

Minimum shrink temperature: 60℃

Minimum full recovery temperature: 100℃

- Standards/Approvals

UL224 E214175 125℃ VW-1

- Specification values

|  | Property | Requirement | Test method | Typical data |
| --- | --- | --- | --- | --- |
| Physical： | Concentricity | 70% min. | ASTM D 2671 | ≥70% |
|  | Tensile strength | 10.4MPa min. | ASTM D 638 | ≥14.0MPa |
|  | Elongation | 200% min. | ASTM D 638 | ≥400% |
|  | Heat shock | No cracking, dripping or flowing | ASTM D 2671 | Pass |
|  | Low temperature flexibility | No cracking | ASTM D 2671 | Pass |
|  | Aging 158℃,168hrs |  |  |  |
|  | Tensile strength after aging | 70% of original min. | ASTM D 638 | ≥90% |
|  | Elongation after aging | 100% min. | ASTM D 638 | ≥300% |
| Electrical： | Dielectric voltage withstand | 2500V, 60sec no breakdown | UL224 | Pass |
|  | Dielectric strength | 19.7kV/mm min. | ASTM D 2671 | 25kV/mm |
|  | Volume resistivity | 1014Ω·cm min. | ASTM D 876 | ≥1014Ω·cm |
| Chemical： | Corrosion | No corrosion | ASTM D 2671 | Pass |
|  | Flammability | VW-1 | UL224 | Pass |

- Product sizes

·Metric size

| Size (mm) | As supplied(mm) | After recovery(mm) | Standard length （m/spool） |
| --- | --- | --- | --- |
|  | Inside diameter | Wall thickness | Inside diameter (max.) | Wall thickness (min.) |  |
| Φ1.0 | 1.4±0.2 | 0.10±0.03 | 0.60 | 0.20 | 200 |
| Φ1.5 | 1.9±0.2 | 0.10±0.03 | 0.75 | 0.20 | 200 |
| Φ2.0 | 2.4±0.2 | 0.12±0.03 | 1.00 | 0.20 | 200 |
| Φ2.5 | 2.8±0.3 | 0.13±0.05 | 1.25 | 0.25 | 200 |
| Φ3.0 | 3.4±0.3 | 0.13±0.05 | 1.50 | 0.25 | 200 |
| Φ3.5 | 3.9±0.3 | 0.13±0.05 | 1.75 | 0.25 | 200 |
| Φ4.0 | 4.4±0.3 | 0.15±0.05 | 2.00 | 0.25 | 200 |
| Φ5.0 | 5.5±0.3 | 0.15±0.05 | 2.50 | 0.25 | 100 |
| Φ6.0 | 6.5±0.3 | 0.15±0.05 | 3.00 | 0.28 | 100 |
| Φ7.0 | 7.5±0.3 | 0.15±0.05 | 3.50 | 0.28 | 200 |
| Φ8.0 | 8.6±0.4 | 0.15±0.05 | 4.00 | 0.28 | 200 |
| Φ9.0 | 9.6±0.4 | 0.15±0.05 | 4.50 | 0.28 | 200 |
| Φ10.0 | 10.6±0.4 | 0.15±0.05 | 5.00 | 0.28 | 200 |
| Φ11.0 | 11.6±0.4 | 0.18±0.05 | 5.50 | 0.28 | 200 |
| Φ12.0 | 12.6±0.4 | 0.20±0.05 | 6.00 | 0.28 | 200 |
| Φ13.0 | 13.6±0.4 | 0.20±0.05 | 6.50 | 0.30 | 200 |
| Φ14.0 | 14.6±0.4 | 0.20±0.05 | 7.00 | 0.30 | 200 |
| Φ15.0 | 15.6±0.5 | 0.20±0.05 | 7.50 | 0.32 | 200 |
| Φ16.0 | 16.6±0.5 | 0.20±0.05 | 8.00 | 0.32 | 200 |
| Φ18.0 | 18.6±0.5 | 0.22±0.05 | 9.00 | 0.36 | 200 |
| Φ20.0 | 21.0±1.0 | 0.25±0.05 | 10.0 | 0.36 | 100 |
| Φ22.0 | 23.0±1.0 | 0.25±0.05 | 11.0 | 0.40 | 100 |
| Φ25.0 | 26.0±1.0 | 0.25±0.05 | 12.5 | 0.40 | 100 |

- Ordering Information

# Color

Standard: Black (-BK), white (-WH), red (- RD), blue (-BL), yellow (-YL), green (-GR)

Nonstandard: Available upon request.

# Nonstandard size

Special sizes are available upon request.

# Standard packaging

On spools. Cut pieces are available upon request.

# Ordering description

Specify product type, size (mm or inch) and color.