GUANZHOU KAIHENG K&S CO.,LTD.

Address:NO.148,Chang'an,Guangshan Road,Huangpu District,Guangzhou,China

TEL:+86-20-3207 9090              FAX:+86-20-3207 9103

E-mail:angel@gzkaiheng.com         URL:www.gzkaiheng.com

weChat / QQ:68118858              Skype:fengfengzhou

Mobile phone/whatsApp:+86-13416189912

KOSOO K-2(3X)

Flexible, flame-retardant, high-shrink-ratio polyolefin tubing

- Application

KOSOO K-2 (3X) is flexible, flame-retardant, high-shrink-ratio irradiated crosslinking heat-shrinkable modified polyolefin tubing. K-2(3X) has 3:1 shrink ratio which is needed to cover larger size differences like harnesses with installed connectors. It is used for insulation protection, bundling or capsule of wire terminals and components with larger size differences.

- Features/Benefits

·Shrink ratio: 3:1.

·Flexible, highly flame-retardant.

·Excellent physical, chemical and electrical properties and high reliability.

·Abrasion and fluids resistance.

·Conform to European RoHS（2002/95/EC） environmental directive.

- Operating Temperature Range

Operating temperature range: -55℃~135℃

Minimum shrink temperature: 70℃

Minimum full recovery temperature: 110℃

- Standards/Approvals

UL224 E214175 125℃ 600V VW-1

AMS-DTL-23053/5 class 2 and class 3

- Specification values

|  | Property | Requirement | Test method | Typical data |
| --- | --- | --- | --- | --- |
| Physical： | Concentricity | 70% min. | ASTM D 2671 | ≥70% |
|  | Tensile strength | 10.4MPa min. | ASTM D 638 | ≥14.0MPa |
|  | Elongation | 200% min. | ASTM D 638 | ≥400% |
|  | Heat shock 250℃, 4hrs | No cracking, dripping or flowing | ASTM D 2671 | Pass |
|  | Low temperature flexibility -55℃, 4hrs | No cracking | ASTM D 2671 | Pass |
|  | Aging 175℃,168hrs |  |  |  |
|  | Tensile strength after aging | 70% of original min. | ASTM D 638 | ≥90% |
|  | Elongation after aging | 100% min. | ASTM D 638 | ≥300% |
| Electrical： | Dielectric voltage withstand | 2500V, 60sec no breakdown | UL224 | Pass |
|  | Dielectric strength | 19.7KV/mm min. | ASTM D 2671 | 25KV/mm |
|  | Volume resistivity | 1014Ω·cm min. | ASTM D 876 | ≥1014Ω·cm |
| Chemical： | Corrosion | No corrosion | ASTM D 2671 | Pass |
|  | Flammability | VW-1 | UL224 | Pass |

- Product sizes

| Size（mm） | As supplied(mm) | After recovery(mm) | Standard length (m/spool)) |
| --- | --- | --- | --- |
|  | Inside diameter | Wall thickness | Inside diameter (max.) | Wall thickness |  |
| 1.5/0.5 | 1.8±0.3 | 0.20±0.05 | 0.5 | 0.50±0.10 | 200 |
| 3/1 | 3.3±0.3 | 0.20±0.05 | 1.0 | 0.60±0.10 | 200 |
| 6/2 | 6.5±0.3 | 0.25±0.05 | 2.0 | 0.70±0.10 | 100 |
| 9/3 | 9.5±0.4 | 0.30±0.06 | 3.0 | 0.80±0.15 | 100 |
| 12/4 | 12.5±0.4 | 0.30±0.06 | 4.0 | 0.85±0.15 | 100 |
| 18/6 | 18.5±0.5 | 0.35±0.06 | 6.0 | 1.00±0.15 | 50 |
| 24/8 | 26.0±1.0 | 0.40±0.10 | 8.0 | 1.20±0.20 | 50 |
| 40/13 | 41.5±1.0 | 0.45±0.10 | 13.0 | 1.25±0.20 | 50 |

- Ordering Information

# Color

Standard: Black (-BK), white (-WH), red (-RD), blue (-BL), yellow (-YL), green (-GR)

Nonstandard: Available upon request.

# Nonstandard size

Special sizes are available upon request.

# Standard packaging

On spools. Cut pieces are available upon request.

# Ordering description

Specify product type, size (mm or inch) and color.