GUANZHOU KAIHENG K&S CO.,LTD.

Address:NO.148,Chang'an,Guangshan Road,Huangpu District,Guangzhou,China

TEL:+86-20-3207 9090              FAX:+86-20-3207 9103

E-mail:angel@gzkaiheng.com         URL:www.gzkaiheng.com

weChat / QQ:68118858              Skype:fengfengzhou

Mobile phone/whatsApp:+86-13416189912

KOSOO K-2(GYS)

Yellow & green striped, flexible, flame-retardant polyolefin tubing

- Application

KOSOO K-2 (GYS) is yellow & green striped, flexible, flame-retardant, irradiated crosslinking heat-shrinkable modified polyolefin tubing. It is designed for use in earth sleeving. 3:1 shrink ratio is for more suitable for application to irregular, awkward shapes.

- Features/Benefits

·Shrink ratio: 2:1, 3:1.

·Flexible, flame-retardant.

·Excellent physical, chemical and electrical properties and high reliability.

·Free of PCBs, PCPs, polybrominated biphenyls (PBBs), polybrominated biphenyl oxides and ethers (PBBOs, PBBEs and PBDEs) and toxic heavy metal compounds, which are classified as environmentally hazardous substances. Conform to European RoHS environmental directive.

- Operating Temperature Range

Operating temperature range: -55℃~135℃

Minimum shrink temperature: 70℃

Minimum full recovery temperature: 110℃

- Standards/Approvals

UL224 E214175 125℃ 600V VW-1

AMS-DTL-23053/5 class 2 and class 3

- Specification values

|  | Property | Requirement | Test method | Typical data |
| --- | --- | --- | --- | --- |
| Physical： | Concentricity | 70% min. | ASTM D 2671 | ≥70% |
|  | Tensile strength | 10.4MPa min. | ASTM D 638 | ≥14.0MPa |
|  | Elongation | 200% min. | ASTM D 638 | ≥400% |
|  | Heat shock | No cracking, dripping or flowing | ASTM D 2671 | Pass |
|  | Low temperature flexibility | No cracking | ASTM D 2671 | Pass |
|  | Aging 158℃,168hrs |  |  |  |
|  | Tensile strength after aging | 70% of original min. | ASTM D 638 | ≥90% |
|  | Elongation after aging | 100% min. | ASTM D 638 | ≥300% |
| Electrical： | Dielectric voltage withstand | 2500V, 60sec no breakdown | UL224 | Pass |
|  | Dielectric strength | 19.7kV/mm min. | ASTM D 2671 | 25kV/mm |
|  | Volume resistivity | 1014Ω·cm min. | ASTM D 876 | ≥1014Ω·cm |
| Chemical： | Corrosion | No corrosion | ASTM D 2671 | Pass |
|  | Flammability | VW-1 | UL224 | Pass |

Product sizes

·Inch size (2:1)

| Size (inch) | As supplied (mm) | After recovery (mm) | Standard length （m/spool） |
| --- | --- | --- | --- |
|  | Inside diameter (min.) | Wall thickness (nominal) | Inside diameter (max.) | Wall thickness (min.) |  |
| 1/16 | 1.6 | 0.20 | 0.8 | 0.36 | 200 |
| 3/32 | 2.4 | 0.25 | 1.2 | 0.44 | 200 |
| 1/8 | 3.2 | 0.25 | 1.6 | 0.44 | 200 |
| 3/16 | 4.8 | 0.25 | 2.4 | 0.44 | 200 |
| 1/4 | 6.4 | 0.30 | 3.2 | 0.56 | 100 |
| 5/16 | 8.0 | 0.30 | 4.0 | 0.56 | 100 |
| 3/8 | 9.5 | 0.30 | 4.8 | 0.56 | 100 |
| 1/2 | 12.7 | 0.35 | 6.4 | 0.56 | 100 |
| 5/8 | 15.9 | 0.38 | 8.0 | 0.68 | 100 |
| 3/4 | 19.1 | 0.40 | 9.5 | 0.77 | 50 |
| 1 | 25.4 | 0.45 | 12.7 | 0.87 | 50 |
| 1 1/2 | 38.1 | 0.50 | 19.0 | 0.97 | 50 |
| 2 | 50.8 | 0.55 | 25.4 | 0.97 | 50 |

·Inch size (3:1)

| Size (inch) | As supplied (mm) | After recovery (mm) | Standard length （m/spool） |
| --- | --- | --- | --- |
|  | Inside diameter (min.) | Wall thickness (nominal) | Inside diameter (max. ) | Wall thickness (min.) |  |
| 1/16 | 1.5 | 0.20 | 0.5 | 0.40 | 200 |
| 3/32 | 2.4 | 0.20 | 0.8 | 0.42 | 200 |
| 1/8 | 3.0 | 0.20 | 1.0 | 0.50 | 200 |
| 3/16 | 4.8 | 0.20 | 1.6 | 0.50 | 200 |
| 1/4 | 6.0 | 0.25 | 2.0 | 0.60 | 100 |
| 3/8 | 9.0 | 0.30 | 3.0 | 0.65 | 100 |
| 1/2 | 12.0 | 0.30 | 4.0 | 0.70 | 100 |
| 3/4 | 18.0 | 0.35 | 6.0 | 0.75 | 50 |
| 1 | 24.0 | 0.45 | 8.0 | 1.00 | 50 |
| 1 1/2 | 39.0 | 0.45 | 13.0 | 1.05 | 50 |

■Ordering Information

# Color

Standard: Yellow & green stripe

Nonstandard: Other dual colors can be available upon request.

# Nonstandard size

Special sizes are available upon request.

# Standard packaging

On spools. Cut pieces are available upon request.

# Ordering description

Specify product type, size (mm or inch) and color.